Government of Pakistan

National Vocational and Technical Training Commission

(NAVTTC)

"Prime Minister Youth Skill Development Program"

Course Contents / Lesson Plan

Course Title: Paint Shop Technician

Course Code: _______________

Duration:  3 Months

| Author Name | Malik Izhar Ahmed Awan, Ihsan Mujtaba, Engr. Muhammad Ali, Ghulam Muheedin Ahmed, Tanvir Akram Awan |
| --- | --- |
| Date of Development | 13-6-2026 |
| Course Title | Paint Shop Technician |
| Training Objective & Learning Outcomes | The objective of a Paint Shop Technician short course for the fan industry is to equip participants with the essential technical skills required to meet the growing demand for skilled labor in this sector. The course focuses on practical training in surface preparation, paint mixing, spray techniques, and finishing processes, ensuring that learners can deliver high-quality, durable coatings for fan components. By emphasizing industry-relevant practices, the program aims to reduce production errors, improve efficiency, and raise the overall standard of workmanship in paint shops. Another key objective is to build a workforce that can adapt to modern technologies and safety standards in industrial painting. Learners will be trained not only in technical application but also in workplace safety, equipment handling, and quality control measures. This holistic approach ensures that graduates are job-ready, capable of contributing immediately to production lines, and able to support the industry in overcoming its shortage of skilled technicians. Ultimately, the course seeks to strengthen the fan industry’s competitiveness by creating a pool of reliable, well-trained professionals. - Learners will be able to properly clean, sand, and prepare fan components for painting. - Participants will understand how to mix paints and coatings to achieve consistent colors and finishes. - Learners will gain hands-on skills in using spray guns and other equipment for smooth, even coatings. - Students will learn methods for polishing, sealing, and ensuring durable finishes. - Graduates will be able to inspect painted components and identify defects or inconsistencies. - Learners will understand safety protocols, including handling chemicals and using protective gear. - Participants will be trained to maintain spray guns, compressors, and other tools for long-term use. - Students will learn how to minimize waste, reduce errors, and improve workflow in the paint shop. - Learners will be introduced to new painting methods and eco-friendly coatings used in the fan industry. - Graduates will develop communication and teamwork skills to work effectively in industrial settings. |
| Entry-level of trainees | Middle |
| Minimum Qualification of Teachers | Matric with 3 years Fain painting Experience |
| Scheme of Studies | Course Title Sr. No; Modules; Theory Hrs.; Practical Hrs.; Total Hrs.. Introduction & Basics of Paint Shop; 5; 20; 25. Surface Selection for Painting; 5; 20; 25. Paint Mixing and Application; 5; 20; 25. Advanced Painting Techniques; 5; 20; 25. Powder Coating; 5; 20; 25. Heating and curing system; 5; 20; 25. Fan specific painting operations; 5; 20; 25. Quality Control (QC); 5; 20; 25. Defect analysis and troubleshooting; 5; 20; 25. Production operations; 5; 20; 25. Safety and environment; 5; 20; 25. Final assessment and evaluation; 5; 20; 25. Total; 60; 240; 300. |
| Course Execution Plan | Duration of the course: 3 months (12 Weeks) Theory: 20% Practical: 80% Weekly hours: 25 hours per week Total contact hours: Maximum 300 hours |
| Companies offering jobs in the respective trade |  |
| No of Students | 25 |
| Learning Place | Classroom /Workplace |
| Instructional Resources | - PDF Books - Video Tutorials etc |

DETAIL OF COURSE CONTENTS

| Module Title | Learning Units | Learning elements | Task/Practical |
| --- | --- | --- | --- |
| Week 1 Introduction & Basics of Paint Shop | Day 1 - Draw paint shop process - Recognize blades, body, and brackets - Map preparation, coating, and drying areas - Observe corrosion protection and aesthetics | - Explain paint shop workflow in fan manufacturing - Enlist fan components used in painting line - Describe paint shop layout and sections - Elaborate importance of painting in industry | Task: Visit the paint shop and observe the complete painting workflow from surface preparation to final inspection. Identify the major sections of the paint shop and the fan components processed in each section. Record your observations and discuss the importance of painting in fan manufacturing. |
|  | Day 2 - Examine coating protection function - Identify components of paint - Analyze drying and bonding process - Differentiate liquid and powder coatings | - Define paint and its purpose - Enlist resin, pigment, solvent, additives - Explain paint film formation - Classify basic paint types | Task: Examine different paint samples used in the paint shop. Identify the basic components of paint by reviewing product labels and technical data sheets. Discuss how each component contributes to coating performance and protection. |
|  | Day 3 - Identify enamel, epoxy, PU, powder - Analyze durability and finish quality - Match coating with metal components - Justify selection for blades and body | - Describe industrial paint types - Elaborate paint properties - Describe paint for fan parts - Explain paint application suitability | Task: Inspect various paint products used for ceiling and pedestal fans. Compare their appearance, drying characteristics, and intended applications. Prepare a comparison chart showing the differences between enamel, epoxy, PU, and powder coatings. |
|  | Day 4 - Identify primer, base, and top coat layers - Analyze bonding between metal and paint - Detect peeling, blistering, and cracks - Evaluate coating durability | - Describe coating system structure - Explain adhesion mechanism - Brief coating defects - Elaborate coating performance | Task: Observe coated fan components and identify the primer, base coat, and top coat layers where applicable. Examine examples of coating defects and discuss possible causes. Record observations on coating performance and appearance. |
|  | Day 5 - Recognize chemical and fire risks - Wear mask, gloves, and goggles - Observe fume extraction operation - Follow entry safety rules | - Elaborate safety hazards in paint shop - Brief PPE usage - Explain ventilation systems - Elaborate safety procedures | Task: Wear the required PPE and demonstrate proper safety practices within the paint shop. Inspect safety signs, emergency exits, and ventilation systems. Report any potential hazards identified during the inspection. |
| Week 2 Surface Selection for Painting | Day 1 - Recognize MS and aluminum parts - Match coating with substrate - Detect rust and damage - Identify scratches and dents | - Explain metal surfaces - Explain surface compatibility - Describe raw materials - Elaborate surface defects | Task: Inspect different fan components made from mild steel and aluminum. Identify surface conditions such as rust, dents, scratches, or contamination. Record findings and determine whether each component is suitable for painting. |
|  | Day 2 - Describe adhesion improvement role - Apply chemical cleaning - Select alkaline or solvent cleaner - Verify oil-free surface | - Explain surface preparation importance - Explain degreasing process - Brief cleaning agents - Define cleaning results | Task: Perform a degreasing operation on selected fan components using approved cleaning materials. Verify that oil and grease have been removed effectively. Inspect the cleaned surface and document the results. |
|  | Day 3 - Explain abrasive cleaning action - Identify pressure settings - Compare blasting vs chemical cleaning - Evaluate surface roughness | - Describe sand blasting process - Explain blasting operation - Explain cleaning methods - Brief blasted surface | Task: Observe or perform a blasting operation under supervision. Compare the surface condition before and after blasting. Evaluate the effectiveness of blasting in preparing the surface for coating. |
|  | Day 4 - Describe chemical conversion coating - List rinsing and activation steps - Evaluate protective layer formation - Arrange process flow correctly | - Explain phosphating process - Elaborate treatment stages - Explain corrosion resistance - Elaborate process sequence | Task: Observe the phosphating process and identify each stage of treatment. Examine treated components and compare them with untreated samples. Discuss how phosphating improves corrosion resistance and paint adhesion. |
|  | Day 5 - Perform rinsing and drying - Identify dust and oil - Verify surface readiness - Record inspection data | - Elaborate surface cleaning methods - Brief contamination sources - Define cleaned surfaces - Elaborate preparation results | Task: Clean and dry prepared fan components according to standard procedures. Inspect surfaces for dust, oil, and other contaminants. Complete an inspection checklist and record the condition of each component. |
| Week 3 Paint Mixing and Application | Day 1 - Calculate mixing ratios - Select stirrers and containers - Adjust thinner quantity - Check flow behavior | - Explain paint mixing process - Elaborate mixing tools - Control paint viscosity - Evaluate consistency | Task: Prepare a paint mixture according to the manufacturer's instructions. Measure the required quantities and mix the materials thoroughly. Check viscosity and record all mixing data. |
|  | Day 2 - Follow mixing procedure - Identify working time - Remove impurities - Maintain consistency | - Define paint batches - Explain pot life - Apply filtration - Ensure uniformity | Task: Prepare a production paint batch and filter it before use. Monitor the working time of the paint and observe any changes in consistency. Record observations regarding pot life and paint quality. |
|  | Day 3 - Identify atomization - Recognize nozzle and air cap - Demonstrate pressure and flow - Apply uniform coating | - Explain spray painting process - Explain spray gun parts - Describe spray settings - Explain spray control | Task: Disassemble and identify the main components of a spray gun. Reassemble the equipment and adjust the operating parameters. Perform a spray pattern test on a practice panel. |
|  | Day 4 - Perform primer application - Measure wet film thickness - Avoid runs and sags - Evaluate finish quality | - Define base coating - Define control coating thickness - Describe to Prevent defects - Explain painted surface | Task: Apply primer coating to a sample fan component or test panel. Measure the wet film thickness and inspect the coating for uniformity. Record any defects observed during application. |
|  | Day 5 - Identify overspray issues - Perform rework operations - Prepare clean spray gun - Document daily production | - Enlist painting errors - Describe to correct coating defects - Describe how to maintain equipment - Explain how to Record production output | Task: Inspect coated panels for common painting defects such as runs, sags, or overspray. Perform corrective actions where necessary. Document the defects and the corrective measures taken. |
| Week 4 Advanced Painting Techniques | Day 1 - Apply primer, base, top coat - Describe coating sequence - Inspect surface smoothness - Ensure consistent finish | - Explain multi-layer coating - Explain coating system - Describe to control finish quality - Explain uniformity | Task: Apply a complete multi-layer coating system consisting of primer, base coat, and top coat. Inspect each layer before applying the next coat. Evaluate the final finish for consistency and appearance. |
|  | Day 2 - Adjust spray angle - Prevent orange peel - Detect uneven coating - Fix surface defects | - Define to improve spray technique - Elaborate how to control paint distribution - Enlist defects - Describe correct coating errors | Task: Adjust spray angles and distances while applying paint to practice panels. Observe the effect of different techniques on coating quality. Record the settings that produce the best finish. |
|  | Day 3 - Coat fan blades evenly - Inspect about control weight distribution - Inspect to reduce paint waste - Prepare to check surface smoothness | - Explain blade coating - Define paint application - Explain how to prevent overspray - Define about finish quality | Task: Apply coating to ceiling fan blades while maintaining uniform coverage. Inspect the blades for even paint distribution and surface quality. Compare finished blades and note any differences. |
|  | Day 4 - Measure coating variation - Modify pressure settings - Test coating strength - Detect surface defects | - Describe about analyze coating thickness - Define how to adjust spray settings - Describe to evaluate adhesion - Define about improve the finishing | Task: Measure coating thickness at multiple locations on painted components. Compare the readings with specified standards. Adjust application parameters if thickness variations are detected. |
|  | Day 5 - Check cosmetic finish - Compare standards - Report defects - Record inspection data | - Explain about demonstrate finishing standards - Define how to Inspect product appearance - Define rework needs - Explain how to document quality issues | Task: Inspect finished fan components according to company quality standards. Identify any cosmetic defects requiring rework. Complete an inspection report and recommend corrective actions. |
| Week 5 Powder coating process | Day 1 - Define powder coating process - Recognize thermoset and thermoplastic powders - Compare powder and liquid paints - Select suitable coating for fan parts | - Explain powder coating principles - Describe powder coating materials - Describe advantages of powder coating - Classify powder coating types | Task: Examine different powder coating materials used in fan manufacturing. Compare their appearance, texture, and application characteristics. Record observations and identify suitable applications for each powder type. |
|  | Day 2 - Recognize spray gun components - Observe powder charging operation - Identify attraction between powder and metal - Follow grounding procedures | - Explain electrostatic coating process - Explain powder coating equipment - Describe powder charging mechanism - Describe electrostatic safety practices | Task: Observe the operation of an electrostatic powder coating system. Identify the major components of the equipment and explain their functions. Verify grounding arrangements and discuss safety requirements. |
|  | Day 3 - Set spray gun parameters - Regulate powder output - Apply uniform coating - Evaluate powder coverage | - Explain how to operate powder coating equipment - Describe the control powder flow - Define application parameters - Define to monitor coating consistency | Task: Operate or observe powder coating equipment while applying powder to sample components. Monitor powder flow and coating coverage throughout the process. Inspect coated parts for uniformity and record results. |
|  | Day 4 - Set oven temperature - Follow curing schedules - Inspect cured surfaces - Verify coating durability | - Explain curing process - Control curing temperature - Monitor curing time - Evaluate coating hardness | Task: Load coated components into the curing oven and monitor the curing cycle. Record temperature and curing time according to the process specification. Inspect cured components for hardness and finish quality. |
|  | Day 5 - Detect pinholes and orange peel - Investigate defect causes - Apply corrective actions - Clean coating equipment | - Define powder coating defects - Analyze causes of coating defects - Explain to correct coating problems - Maintain powder coating equipment | Task: Inspect powder-coated samples for defects such as pinholes, orange peel, or insufficient coverage. Identify possible causes of each defect. Recommend corrective actions and document findings. |
| Week 6 Heating and curing systems | Day 1 - List oven components - Observe heating operation - Identify temperature distribution - Follow heating safety procedures | - Explain heating systems used in paint shops - Explain curing equipment - Describe heat transfer principles - Define heating safety requirements | Task: Inspect the curing oven and identify all major components. Observe heat circulation within the system and discuss how temperature affects coating quality. Record observations regarding safe oven operation. |
|  | Day 2 - Measure oven temperature - Compare readings with standards - Identify temperature fluctuations - Document observations | - Explain to control curing temperature - Explain to monitor oven performance - Describe to analyze temperature variations - Record operating conditions | Task: Measure and record oven temperatures at different locations. Compare readings with standard operating requirements. Discuss possible reasons for temperature variations within the oven. |
|  | Day 3 - Apply standard curing schedules - Monitor process duration - Inspect coating hardness - Verify complete curing | - Explain to set curing cycles - Explain to control curing time - define curing effectiveness - Maintain curing quality | Task: Monitor a complete curing cycle from start to finish. Verify that curing times meet process requirements. Inspect the final coating and record the results. |
|  | Day 4 - Detect under-curing defects - Detect over-curing defects - Recommend corrective actions - Evaluate process improvements | - Explain heat-related coating defects - Define curing problems - Describe to correct curing issues - Explain process efficiency | Task: Evaluate coated samples showing under-cured and over-cured conditions. Identify visible signs of curing defects. Recommend process adjustments to prevent recurrence. |
|  | Day 5 - Calculate energy usage - Compare operating conditions - Record production data - Prepare performance reports | - Explain oven performance - Explain how to assess energy efficiency - Explain to monitor production flow - Document curing results | Task: Review oven performance data and calculate energy usage for a production shift. Compare actual conditions with operational standards. Prepare a brief report summarizing findings and recommendations. |
| Week 7 Fan specific painting operations | Day 1 - Recognize fan housing parts - Prepare components for painting - Apply uniform coating - Inspect painted surfaces | - Explain painting requirements of ceiling fans - Enlist ceiling fan components - Define coating to fan bodies - Maintain coating quality | Task: Prepare ceiling fan bodies for painting by inspecting the surfaces and ensuring they are free from contamination. Apply coating using the approved painting method while maintaining uniform coverage. Inspect the finished surface and record observations related to coating quality and appearance. |
|  | Day 2 - Apply paint evenly - Monitor coating thickness - Check blade balance - Inspect appearance | - Explain paint ceiling fan blades - Explain to control paint distribution - Prevent coating imbalance - Describe the evaluate blade finish | Task: Paint ceiling fan blades according to standard operating procedures. Monitor paint distribution to ensure balanced coating across all blades. Inspect the finished blades for consistency, smoothness, and uniform color. |
|  | Day 3 - Identify pedestal fan parts - Apply coating uniformly - Examine coated surfaces - Verify quality standards | - Explain paint pedestal fan components - Explain to control coating on frames - Explain painted assemblies - Explain finish standards | Task: Apply coating to pedestal fan frames and supporting structures. Pay special attention to corners, joints, and hard-to-reach areas during application. Inspect the coated components and document any defects or areas requiring rework. |
|  | Day 4 - Compare colors with standards - Apply decorative coatings - Inspect finish quality - Correct appearance defects | - Explain decorative finishes - Explain color specifications - define product appearance - Explain finish consistency | Task: Apply decorative finishes and approved color schemes to selected fan components. Compare the finished color with the production standard or sample panel. Record any color variations and recommend corrective actions if required. |
|  | Day 5 - Perform visual inspection - Detect surface defects - Record observations - Recommend corrective actions | - Explain painted fan products - Describe final appearance - Explain quality issues - Define about document inspection findings | Task: Conduct a final visual inspection of painted fan products before assembly. Verify coating quality, appearance, and color consistency. Complete an inspection checklist and document all findings. |
| Week 8 Quality Control (QC) | Day 1 - Define quality standards - Examine coated surfaces - Identify visible defects - Complete inspection records | - Explain quality control requirements - Enlist inspection methods - Define visual inspection techniques - Enlist inspection results | Task: Perform visual inspection on painted fan components using approved quality standards. Identify defects such as scratches, dust particles, uneven coating, or color variations. Record inspection results and classify defects according to company procedures. |
|  | Day 2 - Use DFT gauge - Record thickness values - Analyze measurements - Verify acceptance criteria | - Define coating thickness - Brief thickness gauges - Elaborate results with specifications - Explain coating compliance | Task: Measure dry film thickness on painted components using a DFT gauge. Take readings from multiple locations and compare them with specified requirements. Document all measurements and identify any non-conforming results. |
|  | Day 3 - Conduct cross-hatch test - Observe coating performance - Record findings - Compare with standards | - Explain adhesion testing methods - Brief adhesion tests - Define coating strength - Enlist test results | Task: Conduct an adhesion test on coated samples using the approved test method. Observe coating performance and determine whether adhesion requirements have been achieved. Record test results and discuss possible causes of failure if observed. |
|  | Day 4 - Categorize defects - Investigate root causes - Suggest improvements - Document corrective measures | - Enlist coating defects - Enlist defect causes - Enlist corrective actions - Brief coating quality | Task: Inspect a batch of painted components and categorize defects according to type and severity. Analyze possible root causes for each defect identified. Prepare a corrective action plan to improve coating quality. |
|  | Day 5 - Compile inspection data - Analyze quality trends - Complete reports - Organize documentation | - Explain quality reports - Enlist inspection findings - Elaborate production quality - Enlist quality records | Task: Compile inspection data collected during the week into a quality control report. Summarize major findings, common defects, and corrective actions taken. Present the report for review and discussion. |
| Week 9 Defect analysis and troubleshooting | Day 1 - Recognize blistering and peeling - Categorize defects - Record defect details - Compare defect patterns | - Elaborate common paint defects - Enlist coating failures - Enlist defect characteristics - Enlist observations | Task: Examine painted samples containing common coating defects such as blistering, peeling, cracking, or pinholes. Identify each defect and describe its characteristics. Record observations and discuss likely causes. |
|  | Day 2 - Trace defect sources - Examine process parameters - Assess material quality - Propose corrective actions | - Define root causes of defects - Enlist process conditions - Enlist material issues - Enlist solutions | Task: Investigate a selected coating defect by reviewing process records, surface preparation practices, and application conditions. Determine the root cause of the defect through observation and discussion. Document findings and propose corrective measures. |
|  | Day 3 - Identify preparation errors - Apply corrective measures - Verify adhesion improvement - Record results | - Elaborate surface preparation defects - Define cleaning processes - Brief coating adhesion - Enlist corrective actions | Task: Inspect improperly prepared surfaces and compare them with correctly prepared samples. Identify preparation errors that may affect coating performance. Apply corrective preparation methods and evaluate the results. |
|  | Day 4 - Modify spray settings - Reduce overspray - Improve finish quality - Monitor improvements | - Enlist application defects - Enlist painting parameters - Elaborate coating quality - Explain process effectiveness | Task: Adjust spray gun settings, air pressure, and paint flow rates to correct application-related defects. Apply coating to test panels and compare results before and after adjustment. Record improvements in coating quality |
|  | Day 5 - Analyze defect reports - Compare performance data - Recommend improvements - Document outcomes | - Explain defect trends - Enlist corrective actions - Elaborate process performance - Enlist quality standards | Task: Review defect records from previous production batches. Analyze trends and identify recurring issues affecting product quality. Prepare recommendations to reduce defects and improve process performance. |
| Week 10 Production operations | Day 1 - Trace production sequence - Observe workflow activities - Identify delays - Suggest improvements | - Explain paint shop production flow - Enlist process stages - Explain workflow - Elaborate operational efficiency | Task: Observe the complete production flow within the paint shop from receiving components to final inspection. Identify each process stage and its contribution to product quality. Prepare a process flow chart based on observations. |
|  | Day 2 - Monitor workstations - Assess workload distribution - Identify bottlenecks - Recommend solutions | - Explain production activities - Elaborate resources effectively - Define productivity - Enlist bottlenecks | Task: Monitor activities at different workstations within the paint shop. Evaluate workload distribution and identify bottlenecks affecting productivity. Suggest practical improvements to balance production activities. |
|  | Day 3 - Record output quantities - Calculate efficiency rates - Compare targets and results - Prepare reports | - Explain production output - Enlist production data - Brief efficiency - Enlist records | Task: Collect production output data during a working shift. Calculate daily production figures and compare them with production targets. Record results and discuss factors affecting productivity. |
|  | Day 4 - Follow production plans - Verify schedule compliance - Monitor operations - Record performance | - Elaborate paint shop operations - Enlist production schedules - Explain workflow continuity - Define output quality | Task: Observe coordination between surface preparation, painting, curing, and inspection activities. Identify delays or interruptions affecting workflow. Recommend actions to improve operational efficiency. |
|  | Day 5 - Review productivity data - Calculate KPIs - Identify improvement opportunities - Present findings | - Explain production performance - Enlist key performance indicators - Enlist improvements - Explain operational results | Task: Review production reports and performance indicators for a selected period. Compare actual performance with planned targets. Prepare a summary highlighting strengths, weaknesses, and improvement opportunities. |
| Week 11 Safety and environment | Day 1 - Recognize hazards - Evaluate risk levels - Implement controls - Follow safety procedures | - Identify workplace hazards - Assess safety risks - Apply safety controls - Promote safe practices | Task: Conduct a workplace safety inspection within the paint shop. Identify potential hazards related to chemicals, equipment, electrical systems, and housekeeping. Prepare a report outlining risks and recommended control measures |
|  | Day 2 - Wear PPE correctly - Check PPE condition - Replace damaged PPE - Verify compliance | - Demonstrate PPE usage - Inspect protective equipment - Maintain PPE condition - Enforce safety compliance | Task: Inspect personal protective equipment used by paint shop personnel. Verify that PPE is in good condition and being used correctly. Record observations and recommend improvements where necessary. |
|  | Day 3 - Read safety labels - Organize chemical storage - Use spill prevention methods - Follow MSDS instructions | - Handle chemicals safely - Store chemicals properly - Prevent chemical exposure - Follow handling procedures | Task: Review chemical storage areas and handling procedures. Verify that containers are properly labeled and stored according to safety requirements. Report any unsafe conditions and recommend corrective actions. |
|  | Day 4 - Recognize ignition sources - Use fire extinguishers - Follow evacuation procedures - Participate in drills | - Explain fire safety requirements - Identify fire hazards - Operate fire-fighting equipment - Respond to emergencies | Task: Participate in a fire safety demonstration or emergency response drill. Practice the correct use of fire extinguishers and emergency evacuation procedures. Record observations and discuss lessons learned from the exercise. |
|  | Day 5 - Segregate waste materials - Dispose of waste properly - Monitor environmental compliance - Conduct housekeeping activities | - Manage paint shop waste - Apply environmental practices - Reduce waste generation - Maintain workplace cleanliness | Task: Inspect waste collection and disposal practices within the paint shop. Verify compliance with environmental and housekeeping requirements. Prepare recommendations to improve waste management and workplace cleanliness. |
| Week 12 Final assessment and practical evaluation | Day 1 - Prepare fan components - Conduct cleaning operations - Inspect prepared surfaces - Record results | - Perform complete surface preparation - Apply cleaning procedures - Verify surface readiness - Maintain process standards | Task: Perform complete surface preparation on selected fan components, including cleaning and inspection activities. Verify that surfaces meet painting requirements before coating. Document the preparation process and inspection results. |
|  | Day 2 - Mix paint correctly - Measure viscosity - Filter paint materials - Inspect prepared paint | - Perform paint mixing operations - Prepare coating materials - Control paint properties - Verify paint quality | Task: Prepare paint materials according to the approved formulation and mixing procedure. Measure viscosity and ensure paint quality meets process requirements. Record all mixing parameters and observations. |
|  | Day 3 - Perform spray application - Control coating thickness - Inspect finish quality - Correct minor defects | - Apply coating processes - Operate painting equipment - Maintain coating quality - Evaluate finished surfaces | Task: Apply paint to fan components using the appropriate application method. Control coating thickness and maintain uniform coverage throughout the operation. Inspect the finished coating and correct minor defects where necessary. |
|  | Day 4 - Measure coating thickness - Perform adhesion tests - Complete inspection reports - Verify compliance with standards | - Conduct quality inspections - Perform coating tests - Evaluate product quality - Document inspection findings | Task: Carry out a complete quality inspection on painted components. Measure coating thickness, perform adhesion testing, and conduct visual inspection. Document all results and determine product acceptance status. |
|  | Day 5 - Perform complete painting cycle - Apply safety practices - Demonstrate quality inspection skills - Present assessment outcomes | - Demonstrate paint shop competencies - Complete practical assessment - Evaluate learning outcomes - Present final project results | Task: Complete a full paint shop practical assessment covering surface preparation, paint mixing, application, curing, quality inspection, and safety practices. Demonstrate competency in all major paint shop operations. Present a final summary of activities, findings, and lessons learned during the training program. |

LIST OF MACHINERY / EQUIPMENT

For the Class of 25 Students (3-Month Course)

| S.No | Name of Items | Unit |
| --- | --- | --- |
|  | Air Compressor | As Required |
|  | Spray Booth | As Required |
|  | Spray Gun (2–3 units) | As Required |
|  | Paint Mixing Machine | As Required |
|  | Powder Coating Machine | As Required |
|  | Powder Coating Booth | As Required |
|  | Electric Curing Oven | As Required |
|  | Dry Film Thickness Gauge | As Required |
|  | Adhesion Test Kit | As Required |
|  | Color Matching Cabinet | As Required |
|  | Surface Preparation Tank Set | As Required |
|  | Work Benches | As Required |
|  | Trolleys and Racks | As Required |
|  | Exhaust Ventilation System | As Required |
|  | Complete PPE Sets | As Required |

LIST OF CONSUMABLE MATERIAL

For the Class of 25 Students (3-Month Course)

| S.No | Name of Items | Unit |
| --- | --- | --- |
|  | Primer | 15–20 Liters |
|  | Enamel Paint | 20–25 Liters |
|  | PU Paint | 10–15 Liters |
|  | Thinner | 15–20 Liters |
|  | Powder Coating Powder | 20–50 kg |
|  | Degreasing Chemical | 20 Liters |
|  | Phosphating Chemical | 15 Liters |
|  | Sandpaper Sheets | 100–150 Pieces |
|  | Masking Tape | 30–40 Rolls |
|  | Disposable Gloves | 100 Pairs |
|  | Respirator Masks | 50–100 Pieces |
|  | Metal Practice Panels | 100–150 Pieces |

Trade Registration Form

- Title of the Qualification.

Paint Shop Technician

- List of Competencies/Modules

| Sr.No. | Competency Standards/ Modules |
| --- | --- |
| 1 | Introduction & Basics of Paint Shop |
| 2 | Surface Selection for Painting |
| 3 | Paint Mixing and Application |
| 4 | Advanced Painting Techniques |
| 5 | Powder Coating |
| 6 | Heating and curing system |
| 7 | Fan specific painting operations |
| 8 | Quality Control (QC) |
| 9 | Defect analysis and troubleshooting |
| 10 | Production operations |
| 11 | Safety and environment |
| 12 | Final assessment and evaluation |

- Class / Workshop Size/ Dimension (25 Students Capacity)

|  | Requirement | Size/Dimensions(feet) |
| --- | --- | --- |
| Classroom size | Yes | 25x30 |
| Workshop/Laboratory size | Yes | 25*20 |
| Any other Requirement | No | No |

- Student Teacher Ratio

25:1

- Teacher Qualification: Matric with 3 years Fain painting Experience

- Trainee Eligibility: Middle

- Duration / Credit Hours / Contact Hours

| Contact Hours | Duration |
| --- | --- |
| 300 | 3 months |

- Any other co-curricular activities

| Activity | Requirement |
| --- | --- |
| Industry Linkage | Yes |
| Teacher Training | Yes |
| Workshops and Seminars | Yes |