|  | Assessment Evidence Guide For Jewellery Electroplater 6th-Month Summative Assessment |
| --- | --- |
|  | Date 19th -23rd August, 2024 Lahore |
|  | National Vocational & Technical Training Commission |

Instruction Sheet for the Candidate

| Qualification | National Vocation Certificate Jewellery Electroplater (6th -Month) |
| --- | --- |
| Competency Standard | - Comply With Personal Health and Safety Guidelines - Perform Pre-Treatment of Jewellery Article - Perform Electroplating of Jewellery Article - Perform Post-Treatment of Plated Article - Recover Precious Metals - Develop Entrepreneurial Skills - Adopt Soft Skills |
| Purpose of Assessment | Summative Assessment |
| Candidate Details | Name______________________________________________________ Registration/Roll Number_______________________________________ |
| Guidance for Candidate | To meet this standard, you are required to complete the following within 05 Hrs. time frame (for practical demonstration & assessment): Assessment Task 1: Candidate is required to electroplate complete Jewellery set including bracelet, ring, nose pin, earrings, and necklace including following techniques as per instructions: - Pre-treatment and polishing - Electroplating of gold - Pen Plating of rhodium |
| Time: 05 Hrs. | During a practical assessment, under observation by an assessor, you are required to |
| Minimum Evidence Required | - Wear PPE according to job requirements. - Check for any surface defects including marks, scratches and roughness - Perform deburring/buffing to polish surface of Jewellery article - Fix article in jig and clean Jewellery article using ultrasonic machine for required time - Fix the article in jig and clean Jewellery article using acidic/alkali cleaning bath for required time. - Connect Jewellery article with electrode in electrolytic cleaning apparatus. - Adjust electric current and voltage parameters. - Fix the article in jig and clean Jewellery article using acidic cleaning bath for the required time. - Fix the article in jig and perform electroless plating of Jewellery article as per requirement. - Rinse article with distilled water to remove cleaning media. - Set operating parameters (temperature, pH, voltage, and current density) as per requirement of the article. - Adjust anode/cathode surface area ratio. - Connect electrodes with power supply. - Immerse Jewellery article in electroplating bath. - Perform electroplating (Copper, Nickel, Silver, Gold, Palladium, Platinum, and Rhodium etc.) - Set operating parameters of pen plating unit. - Dip the tip of plating pen into electroplating solution. - Mark the parts of Jewellery article with the help of plating pen’s tip where plating is required. - Rinse article with distilled water to remove electrolyte - Perform electrophoretic protective coating - Cure protective coating by heat drying. - Store chemicals according to compatibility list |
|  | Portfolios required at the time of assessment (if any) for Recover Precious Metals - Perform metal precipitation using proprietary reducing agents. - Perform melting of jigs’ waste into single metallic bar/ingot - Filter and dry precipitated silver powder. Develop Entrepreneurial skills - Compile the information collected through the market survey, in the business plan format. - Prepare marketing plan for new business Plan Industry Visit - Compile all information with pictures in report |

Self-Assessment Checklist

| Candidate Name |  |
| --- | --- |
| Registration No. |  |
| Qualification | National Vocation Certificate Jewellery Electroplater (6th -Month) |
| Competency Standard | - Comply With Personal Health and Safety Guidelines - Perform Pre-Treatment of Jewellery Article - Perform Electroplating of Jewellery Article - Perform Post-Treatment of Plated Article - Recover Precious Metals - Develop Entrepreneurial Skills - Adopt Soft Skills |
| Purpose of Assessment | Summative Assessment |
| Assessment Task | - Electroplate complete Jewellery set including bracelet, ring, nose pin, earrings, and necklace including following techniques as per instructions: - Pre-treatment and polishing - Electroplating of gold - Pen Plating of rhodium - Portfolio |

I can……………….

| Performance Criteria | Yes | No |
| --- | --- | --- |
| - Wear PPE according to job requirements. |  |  |
| - Check for any surface defects including marks, scratches and roughness |  |  |
| - Perform deburring/buffing to polish surface of Jewellery article |  |  |
| - Fix article in jig and clean Jewellery article using ultrasonic machine for required time |  |  |
| - Fix the article in jig and clean Jewellery article using acidic/alkali cleaning bath for required time. |  |  |
| - Connect Jewellery article with electrode in electrolytic cleaning apparatus. |  |  |
| - Adjust electric current and voltage parameters. |  |  |
| - Fix the article in jig and clean Jewellery article using acidic cleaning bath for the required time. |  |  |
| - Fix the article in jig and perform electroless plating of Jewellery article as per requirement. |  |  |
| - Rinse article with distilled water to remove cleaning media. |  |  |
| - Set operating parameters (temperature, pH, voltage, and current density) as per requirement of the article. |  |  |
| - Adjust anode/cathode surface area ratio. |  |  |
| - Connect electrodes with power supply. |  |  |
| - Immerse Jewellery article in electroplating bath. |  |  |
| - Perform electroplating (Copper, Nickel, Silver, Gold, Palladium, Platinum, and Rhodium etc.) |  |  |
| - Set operating parameters of pen plating unit. |  |  |
| - Dip the tip of plating pen into electroplating solution. |  |  |
| - Mark the parts of Jewellery article with the help of plating pen’s tip where plating is required. |  |  |
| - Rinse article with distilled water to remove electrolyte |  |  |
| - Perform electrophoretic protective coating |  |  |
| - Cure protective coating by heat drying. |  |  |
| - Store chemicals according to compatibility list |  |  |
| - Perform metal precipitation using proprietary reducing agents. |  |  |
| - Perform melting of jigs’ waste into single metallic bar/ingot |  |  |
| - Filter and dry precipitated silver powder. |  |  |
| - Compile the information collected through the market survey, in the business plan format. |  |  |
| - Prepare marketing plan for new business |  |  |
| - Compile all information with pictures in report |  |  |

Candidate’s Signature__________________ Assessor’s Signature____________________

Date: ______________________________

Assessors Judgment Guide

| Qualification | National Vocation Certificate Jewellery Electroplater (6th -Month) |
| --- | --- |
| Competency Standard | - Comply With Personal Health and Safety Guidelines - Perform Pre-Treatment of Jewellery Article - Perform Electroplating of Jewellery Article - Perform Post-Treatment of Plated Article - Recover Precious Metals - Develop Entrepreneurial Skills - Adopt Soft Skills |
| Purpose of Assessment | Summative Assessment |
| Candidate Details | Name: ______________________________________________________________ Registration/Roll Number: ______________________Signature: _______________ |
| Assessment Outcome | COMPETENT NOT YETCOMPETENT Name of the Assessor________________________________________________ Assessor’s code: ____________________________________________________ Signature: ________________________________ |

| Assessment Summary (to be filled by the assessor) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Activity | Method |  |  |  |  | Result |  |
| Nature of Activity | Written | Oral | Observation | Portfolio | Role Play | Competent | Not Yet Competent |
| Practical Skill Demonstration |  |  |  |  |  |  |  |
| Knowledge Assessment |  |  |  |  |  |  |  |
| Other Requirement |  |  |  |  |  |  |  |

Observation Checklist

| Assessment Task |  | 1. Electroplate complete Jewellery set including bracelet, ring, nose pin, earrings, and necklace including following techniques as per instructions: - Pre-treatment and polishing - Electroplating of gold - Pen Plating of rhodium 2. Portfolio |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| During the practical assessment, candidate demonstrated the following: |  |  |  | Yes | No | Remarks |
|  | Wear PPE according to job requirements. |  |  |  |  |  |
|  | Check for any surface defects including marks, scratches and roughness |  |  |  |  |  |
|  | Perform deburring/buffing to polish surface of Jewellery article |  |  |  |  |  |
|  | Fix article in jig and clean Jewellery article using ultrasonic machine for required time |  |  |  |  |  |
|  | Fix the article in jig and clean Jewellery article using acidic/alkali cleaning bath for required time. |  |  |  |  |  |
|  | Connect Jewellery article with electrode in electrolytic cleaning apparatus. |  |  |  |  |  |
|  | Adjust electric current and voltage parameters. |  |  |  |  |  |
|  | Fix the article in jig and clean Jewellery article using acidic cleaning bath for the required time. |  |  |  |  |  |
|  | Fix the article in jig and perform electroless plating of Jewellery article as per requirement. |  |  |  |  |  |
|  | Rinse article with distilled water to remove cleaning media. |  |  |  |  |  |
|  | Set operating parameters (temperature, pH, voltage, and current density) as per requirement of the article. |  |  |  |  |  |
|  | Adjust anode/cathode surface area ratio. |  |  |  |  |  |
|  | Connect electrodes with power supply. |  |  |  |  |  |
|  | Immerse Jewellery article in electroplating bath. |  |  |  |  |  |
|  | Perform electroplating (Copper, Nickel, Silver, Gold, Palladium, Platinum, and Rhodium etc.) |  |  |  |  |  |
|  | Set operating parameters of pen plating unit. |  |  |  |  |  |
|  | Dip the tip of plating pen into electroplating solution. |  |  |  |  |  |
|  | Mark the parts of Jewellery article with the help of plating pen’s tip where plating is required. |  |  |  |  |  |
|  | Rinse article with distilled water to remove electrolyte |  |  |  |  |  |
|  | Perform electrophoretic protective coating |  |  |  |  |  |
|  | Cure protective coating by heat drying. |  |  |  |  |  |
|  | Store chemicals according to compatibility list |  |  |  |  |  |
|  | Perform metal precipitation using proprietary reducing agents. |  |  |  |  |  |
|  | Perform melting of jigs’ waste into single metallic bar/ingot |  |  |  |  |  |
|  | Filter and dry precipitated silver powder. |  |  |  |  |  |
|  | Compile the information collected through the market survey, in the business plan format. |  |  |  |  |  |
|  | Prepare marketing plan for new business |  |  |  |  |  |
|  | Compile all information with pictures in report |  |  |  |  |  |
| Competent |  |  | Not yet Competent |  |  |  |

Knowledge Assessment

| Qualification | National Vocation Certificate Jewellery Electroplater (6th -Month) |
| --- | --- |
| Competency Standard | - Comply With Personal Health and Safety Guidelines - Perform Pre-Treatment of Jewellery Article - Perform Electroplating of Jewellery Article - Perform Post-Treatment of Plated Article - Recover Precious Metals - Develop Entrepreneurial Skills - Adopt Soft Skills |
| Purpose of Assessment | Summative Assessment |
| Candidate Details | Name: ______________________________________________________________ Registration/Roll Number: _________________ Candidate Signature: ___________ |
| Assessment Outcome | COMPETENT NOT YETCOMPETENT Name of the Assessor: ________________________________________________ Assessor’s code: ____________________________________________________ Signature of the Assessor: _______________________ |

Candidate’s response is not required to be identical, but similar concepts and/or keywords must be used. Oral questioning may be used to clarify candidate understanding of topic and its application.

| Questions (Candidate confidently answered questions correctly and demonstrated understanding of the topics and their application) |  | Satisfactory | Not Satisfactory |  |
| --- | --- | --- | --- | --- |
|  | What does the red section of the NFPA fire diamond diagram represent? |  |  |  |
|  | What does “3” in the blue section of the NFPA fire diamond diagram indicates? |  |  |  |
|  | What types of contaminants are typically removed during acid/alkali cleaning in the pre-treatment process? |  |  |  |
|  | Why is rhodium commonly used for plating on diamond Jewellery? |  |  |  |
|  | What are the common materials used in inorganic protective coatings for electroplated jewelry? |  |  |  |
| Feedback to the Candidate |  |  |  |  |
| Candidate’s Signature__________________ Assessor’s Signature _________________ |  |  |  |  |

Answer Key

| - What does the red section of the NFPA fire diamond diagram represent? | It represents flammability hazard of the chemical. |
| --- | --- |
| - What does “3” in the blue section of the NFPA fire diamond diagram indicates? | It indicates a serious health hazard, meaning that short exposure could cause temporary or moderate residual injury. |
| - What types of contaminants are typically removed during acid/alkali cleaning in the pre-treatment process? | Oxides, scales, rust, and organic residues |
| - Why is rhodium commonly used for plating on diamond Jewellery? | Rhodium is used for its high reflectivity, hardness, and ability to enhance the brightness and durability of diamond Jewellery. |
| - What are the common materials used in inorganic protective coatings for electroplated jewelry? | silica, alumina, and titanium dioxide |