Course / Subject Name: NQ-Mech-332. Material Testing and Heat Treatment

Assessment Task (Summative Assessment)

A. Perform the following tests on metalic specimen:

1.  Tensile test

2.  Hardness test

OR

B.  Perform the following Non-Destructive Tests (NDT)

1. Visual inspection

OR

C. Perform the following Heat Treatment processes on steel

1. Annealing

2. Quenching

- Performance Criteria for Test 1:

•	Follow safety protocol in each step

•	Adaptive Green practices

•	Arrange the tools and equipment

•	Prepare the specimen (mild steel rod) as per ASTM

•	Ensure the UTM is in working condition

•	Mount the specimen between upper and lower jaws of UTM firmly

•	Attach Extensometer as per UTM manual

•	Apply the load on the specimen

•	Record the values (load, change bin area, change in length)

•	Calculate stress strain

•	Draw stress strain diagram on graph paper

- Performance Criteria for Test 2:

•	Follow safety protocol in each step

•	Adaptive Green practices

•	Arrange the tools and equipment

•	Prepare the specimen as per ASTM

•	Color /Etch the indent ball to make the indentation diameter visible

•	Apply load /pressure for specific time (dwell time) according to material requirement.

•	Note the load /pressure.

•	Measure diameter of indent with microscope

•	calculate the average diameter

•	Calculate hardness using Brinell Hardness Number formula.

•	Record results

B.  Perform the following Non-Destructive Tests (NDT)

visual inspection

Performance Criteria for Test 1:

•	Follow safety protocol in each step

•	Adaptive Green practices

•	Arrange the tools and equipment

•	Select the sample

•	Perform pre-cleaning of sample

•	Apply dye penetrant

•	Remove excess dye penetrant.

•	Apply developer.

•	Inspect specimen for defects.

•	Analyze the sample

•	Interpret the results

C. Perform the following Heat Treatment processes on steel

1. Annealing

2. Quenching

Performance Criteria for Task 1 :

•	Follow safety protocol in each step

•	Adaptive Green practices

•	Arrange the tools and equipment

•	Prepare the sample

•	Preheat the furnace (800 C -900 C)

•	Put the sample in the furnace carefully

•	Heated up to the required temperature

•	Cool the sample in the furnace

•	Take out the sample from furnace

•	Inspect the sample

Performance Criteria for Task 2 :

•	Follow safety protocol in each step

•	Adaptive Green practices

•	Arrange the tools and equipment

•	Prepare the sample

•	Preheat the furnace (800 – 900 0C)

•	Prepare Quenching Medium (oil/water)

•	Put the sample in the furnace carefully

•	Heat the sample up to the required temperature

•	Take out the sample from the furnace

•	Put the sample in the Quenching medium

•	Cool the sample in the Quenching medium

•	Inspect the sample